## Slide 1: Industrial Training at CSIR –NAL
Radhika N.K. M110413EE

## Slide 2: Company profile
National Aerospace Laboratory (NAL)
- premiere research institute under CSIR
Established : 1959
Headquarters: Bangalore
Mission:
-Development of national strengths in aerospace sciences and technologies, infrastructure, facilities and expertise
-Advanced technology solutions to national aerospace programmes.
-Civil aeronautics development
Logo

## Slide 3: Facilities visited
Industrial Fibre Research Facility (IFRF)
Flight Mechanics and Control Division (FMCD)
Aerospace Electronics and Systems Division (AESD)
Advanced Composites Division (ACD)
Electrical Division

## Slide 4: IFRF
Indigenous technology for manufacturing carbon fibre
Pilot plant with capacity 20 TPA.
Technology transferred to Kemrock Industries and Exports Ltd. (KIEL) in 2010
India’s first and only commercial carbon fibre manufacturing plant with 350 TPA capacity by KIEL
Current focus:
Higher modulus carbon fibre for space applications.

## Slide 5: Carbon fibre
Fibres 5-10µm in diameter made mostly of carbon atoms
High tensile strength
High modulus
Low density
Reasonable cost
high chemical resistance
high temperature tolerance
low thermal expansion

## Slide 6: Uses of Carbon fibre

## Slide 7: The Process
Polymerization section
Acrylonitrile +co monomers  Polyacrylonitrile (PAN)
Spinning section
PAN stretched and spun into fibres
Heat treatment section
PAN carbon fibre

## Slide 8: Polymerization section
Acrylonitrile + comonomer
CSTR
Rotary Vaccum Paddle dryer
Dry powder
Centrifuge feed tank
Monomer stripping

## Slide 9: Polymerization reaction in CSTR

## Slide 10: Spinning section
Dry polymer
Granulator
Drying and winding(135oC)
Spinnerette
Coagulation bath(30oC)
Spin dope (60-65oC)
Rollers (stretching)

## Slide 11: Heat treatment section
Stabilization
PAN precursor
Carbon fibre
Graphitization
Surface treatment
Sizing bath

## Slide 12
Stabilization
Oxidation in multizone oven
220oC - 300oC
Line speed 40-50m/h
Product :PANOX
PANOX –fire resistant material
Roller speeds controlled by AC drives
Carbonization
L T furnace
Filled with nitrogen
6 temperature zones
300oC - 900oC gradually
Heating element Kanthal
PID control for temperature

## Slide 13: High temperature processing
As temperature increases, modulus increases
Strength maximum at 1500oC
2 individually controlled zones with graphite elements situated above
Furnace filled with nitrogen
Cooling jackets near bus bars and power feeders (50oC)

## Slide 14
Surface treatment
3 electrolytic treatment cells
2 wash cells
Oil heated drying rollers
Sizing bath
immersion in bath of 0.5% epoxy resin

## Slide 15: Plant Control
DCS
ABB Freelance 2000 series
1000 inputs
AF800 series controllers are used
Protocols
Operator, Process and Engineering stations linked by Ethernet.
CPU modules and I/O modules linked by CAN
Modbus links certain subsystems via RS485 interface

## Slide 16
Control builder F is the software used for configuration of DCS.
Controller tuning done mostly on trial and error basis. No comprehensive tuning strategy executed as yet.

## Slide 17: Energy saving measures
Electric power
APFC panel of 360 kVAR installed. Pf close to unity
Thermal power
3TPH boiler used for process steam at 7 kg/cm2
Demineralized water used to prevent scaling
Economizer used to transfer heat from flu gas to feed water.

## Slide 18: Proposals
Implement Model predictive control as tuning strategy
Bottoming cycle Cogeneration scheme
Hindrances:
Intermittent nature of plant operation
Toxic nature of flue gases
Research facility

## Slide 19: Thank you